

**SE 9393 Stone Effects**

**Product Information\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

The SE 9393 has improved stiffness and good color definition. The SE 9393 also is UV stabilized with FDA compliance is available.

**General Information\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_**

|  |  |
| --- | --- |
| Material Status | Commercial: Active |
| Availability | FDA Compliant Formulations Available |
| Additive | UV stabilized |
| Appearance | Colors Available |
| Forms | Pellets and Powder |
| Processing Method | Rotational Molding |

**Physical Information\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_English Unit\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_\_Test Method\_\_\_\_**

|  |  |  |
| --- | --- | --- |
| Melt Index | 3.5 G/10 MIN | ASTM D-1238 |
| Density | .942 G/CC | ASTM D-1505 |
| Tensile .125” Thick | 2,900 PSI | ASTM D-638 |
| Flexural Modulus 1% Strain | 101,000 PSI | ASTM D-790 |
| Arm Cold (-40°F) Temperature Impact 0.125” Specimen | 40 FT/LB | ARM METHOD |
| ESCR Hours F 50 (100% IGEPAL) | >1,000 | ASTM D-1693 CONDITION A |
| Ultimate Elongation | 500 | \* |

FOR YOUR PROTECTION

THE INFORMATION AND RECOMMENDATIONS IN THIS PUBLICATION ARE TO THE BEST OF OUR KNOWLEDGE AND ARE RELIABLE.  SUGGESTIONS CONCERNING USES OR APPLICATIONS ARE ONLY THE OPINION OF JERICO PLASTIC INDUSTRIES, INC. AND USERS SHOULD MAKE THEIR OWN TESTS TO DETERMINE THE SUITABILITY OF THIS PRODUCT FOR THEIR PARTICULAR PURPOSES.  HOWEVER, BECAUSE OF NUMEROUS FACTORS AFFECTING RESULTS, JERICO PLASTIC INDUSTRIES, INC. MAKES NO WARRANTY OF ANY KIND, EXPRESSED OR IMPLIED.  INCLUDING THOSE OF MERCHANTABILITY AND FITNESS PURPOSES OTHER THAT THE MATERIAL CONFORMS TO ITS APPLICABLE CURRENT STANDARD SPECIFICATIONS.  STATEMENTS HEREIN SHOULD NOT BE CONSTRUED AS REPRESENTATIONS OF WARRENTIES. THE RESPONSIBILTY OF JERICO PLASTIC INDUSTRIES, INC FOR CLAIMS ARISING OUT OF BREECH WARRANTY, NEGLIGENCE, STRICT LIABILITY, OR OTHERWISE IS LIMITED TO THE PURCHASE PRICE OF THE MATERIAL.